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ZEN CARBON PRODUCT CATALOGUE

Product Code
ZEN-[Category Code]-[Thickness(mm)]-[Length(mm)]-[Width(mm)]-[Strength Class]-[Finish/Color Code]
	Category
	Code
	Example

	Paving Block
	PB
	ZEN-PB-60-200-100-C35-GRY

	Hollow Block
	HB
	ZEN-HB-200-400-200-C7.5-GRY

	Solid Block
	SB
	ZEN-SB-150-400-200-C10-GRY

	Hollow Pot Block
	HP
	ZEN-HP-230-380-200-C10-GRY



PAVING BLOCKS
	SKU
	Product Type
	Dimensions (mm)
	Thickness (mm)
	Strength (N/mm²)
	Color / Finish
	Typical Use
	Price (KES/m²)
	Notes              

	ZEN-PB-50-200-100-C25-GRY
	Quad Paver
	200×100
	50
	25
	Grey
	Pedestrian walkways, light duty
	1150/m²
	Medium Duty

	ZEN-PB-60-200-100-C35-GRY
	Quad Paver
	200×100
	60
	35
	Grey
	Driveways, domestic parking
	950–1,100/m²
	Most popular paver size

	ZEN-PB-80-200-100-C49-GRY
	Quad Paver Heavy Duty
	200×100
	80
	49
	Grey
	Industrial/road pavements
	1,150–1,350/m²
	Heavy duty

	ZEN-PB-60-200-165-C35-RED
	Behaton / Uni Paver
	200×165
	60
	35
	Red
	Decorative driveways
	1,100–1,250/m²
	Interlocking, aesthetic

	ZEN-PB-80-200-165-C49-GRY
	Behaton Heavy
	200×165
	80
	49
	Grey
	Heavy duty / parking
	1,300–1,450/m²
	Common for malls

	ZEN-PB-60-205-195-C35-BLK
	Hexagon Paver
	205×195
	60
	35
	Black
	Decorative areas, plazas
	1,200–1,400/m²
	Elegant finish

	ZEN-PB-60-100-100-C35-NAT
	77 Square Paver
	100×100
	60
	35
	Natural
	Garden / pedestrian
	1,000–1,200/m²
	Compact grid pattern

	ZEN-PB-60-330-110-C49-GRY
	Pavia Paver
	330×110
	60
	49
	Grey
	High-end pavements
	1,300–1,500/m²
	Premium grade

	ZEN-PB-60-PIAZZA-SET-C49-MIX
	Piazza Set (Mixed Sizes)
	250–500×150–300
	60
	49
	Mixed
	High-end commercial
	1,500–1,800/m²
	For upscale designs
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MASONRY BLOCKS — HOLLOW & SOLID
	SKU
	Product
	Dimensions (mm)
	Thickness (mm)
	Strength (MPa)
	Weight (kg)
	Use
	Price (KES/block)
	Price (KES/m²)*

	ZEN-HB-100-400-200-C7.5-GRY
	Hollow Block 4"
	390×90×190
	90
	7.5
	12
	Partition walls
	55–65
	1,700–1,900

	ZEN-HB-150-400-200-C10-GRY
	Hollow Block 6"
	390×140×190
	140
	10
	15
	External walls (light duty)
	65–75
	1,850–2,100

	ZEN-HB-200-400-200-C15-GRY
	Hollow Block 9"
	390×190×190
	190
	15
	18
	Load-bearing walls
	75–90
	2,000–2,400

	ZEN-SB-100-400-200-C10-GRY
	Solid Block 4"
	390×90×190
	190
	10
	14
	Internal partition
	60–70
	1,850–2,000

	ZEN-SB-150-400-200-C15-GRY
	Solid Block 6"
	390×140×190
	140
	15
	18
	External wall
	70–85
	2,100–2,400

	ZEN-SB-200-400-200-C20-GRY
	Solid Block 9"
	390×190×190
	190
	20
	24
	Load-bearing wall
	85–100
	2,400–2,800


*Approximate 25 blocks/m² for 4", 20/m² for 6", 15/m² for 9" walling (with mortar).

 HOLLOW POT BLOCKS (RIBBED SLAB INFILL)
	SKU
	Product
	Dimensions (mm)
	Weight (kg)
	Strength (MPa)
	Typical Use
	Price (KES/block)

	ZEN-HP-200-380-200-C10-GRY
	Hollow Pot Block (Standard)
	380×200×200
	8
	10
	Light slabs
	85–95

	ZEN-HP-230-380-200-C10-GRY
	Hollow Pot Block (Medium)
	380×200×230
	9
	10
	Medium spans
	95–105

	ZEN-HP-300-380-200-C10-GRY
	Hollow Pot Block (Heavy)
	380×200×300
	11
	10
	Long-span floors
	110–130




 COLOR / FINISH ADDERS
	Finish
	Code
	Add-on (%)
	Typical Application

	Red oxide
	RED
	+10%
	Driveways, estates

	Black / Charcoal
	BLK
	+12%
	Luxury pavements

	Yellow / Sand
	YLW
	+8%
	Garden paths

	Natural Grey
	GRY
	Base price
	Default



STRENGTH CLASS / QUALITY CONTROL
	Code
	Strength
	Application
	Lab Test Frequency

	C25
	25 N/mm²
	Walkways
	1 batch / 3 days

	C35
	35 N/mm²
	Driveways
	1 batch / 2 days

	C50
	49 N/mm²
	Roads / Industrial
	Every production day

	C7.5
	7.5 MPa
	Non-load walls
	Every 500 pcs

	C10
	10 MPa
	General walls
	Every 500 pcs

	C15
	15 MPa
	Load-bearing
	Daily QC sample
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TYPE INTERLOCK 50mm

SIZE 200 mm x 100 mm x 50 mm
WEIGHT 2 Kgs

PACKING 10 Sg mt =500 pcs.
COMPRESSIVE STRENGTH | 25N/mm?

GRADE Light Duty - KS 827: 2003
TYPE INTERLOCK 60mm

SIZE 200 mm x 100 mm x 60 mm
WEIGHT 2.5 Kgs

PACKING 10 Sg mt = 500 pcs.
COMPRESSIVE STRENGTH | 35N/mm?

GRADE Medium Duty - KS 827: 2003
TYPE INTERLOCK 80mm

SIZE 200 mm x 100 mm x 80 mm
WEIGHT 4kgs

PACKING 10 Sg mt = 500 pcs.
COMPRESSIVE STRENGTH | 49N/mm?

PACKING Heavy Duty - KS 827: 2003
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TYPE QUAD 50 mm

SIZE 200 mm x 100mm x 50mm
WEIGHT 2 Kgs

PACKING 10 Sq mt =500 pcs.
COMPRESSIVE STRENGTH | 35N/mm?

GRADE Medium Duty - KS 827: 2003
TYPE QUAD 60 mm

SIZE 200 mm x 100mm x 60mm
WEIGHT 3 Kgs

PACKING 10 Sq mt = 500 pcs.
COMPRESSIVE STRENGTH | 35N/mm?

GRADE Medium Duty - KS 827: 2003
TYPE QUAD 80 mm

SIZE 200 mm x 100mm x 80mm
WEIGHT 4 Kgs

PACKING 10 Sq mt = 500 pcs.
COMPRESSIVE STRENGTH | 49N/mm?

GRADE Heavy Duty - KS 827: 2003





